| Aromatic Chemical Resistance- |  |
| --- | --- |

| R=Recommended |  | Test Procedure: ASTM D1308 25oC Exceeds 1 Year Test Media |  |
| --- | --- | --- | --- |
| C=Recommended Conditionally (washdown within 1 hour of spillage) |  | Acetone Antifreeze | C R |
| N=Not Recommended |  | Benzene | R |
| 1=Suitable for immersion and/or splash and spillage conditions |  | Benzoic Acid Butyl Alcohol | R R |
| 2=Suitable for occasional or intermittent contact for up to 72 hours |  | Butyl Cellosolve Carbon Dioxide Calcium Hypochlorite | R R N |
| Test Procedure: ASTM D3912 25oC Exceeds 1 Year________________ Test Media |  | Chlorine (5000 ppm in water) Citric Acid Cylloexanol | 2 R R |
| Acetic Acid 10% | C | Dichloacetic Acid | C |
| Ammonium Hydroxide 10%/20 | R | Dimethyl Formamide | N |
| Diesel Fuel | R | Ethanol | 2 |
| Gasoline | R | Ethylene Glycol | 1 |
| Hydraulic Fluid | R | Gasoline | R |
| Hydrochloric Acid 5%/10% | R | Hexane | R |
| Methanol | R | Hydraulic Oil | R |
| Motor Oil | R | Lactic Acid 10% | 1 |
| MTBE | R | Methylene Chloride | C |
| MTBE/Gasoline 5% | R | Methyl Ethyl Ketone | C |
| NaCl/Water 10% | R | Methanol | R |
| Phosphoric Acid 10% | R | Mineral Spirits | R |
| Potassium Hydroxide 10%/20% | R | Monobutyl Ether | R |
| Sodium Hydroxide 10%/20%/50% | R | Nitric Acid 20% | C |
| Sugar/Water 10% | R | Phenol | 2 |
| Sulfuric Acid 5%/10% | R | Skydrol | 2 |
| Skydrol | 2 | Sodium Bicarbonate | R |
| Toluene | C | Sodium Chloride | R |
| Water | R | Sodium Hydroxide 50% | R |
| 2-Methylbutane | R | Sodium Hypochlorite 10% | 2 |
|  |  | Stearic Acid Sulfuric Acid 70% | R N |
| Test Procedure: ASTM B117, after 1000 hours |  | Trichloroethylene | C |
| Test | Result | Trisodium Phosphate Toluene Vinegar | R C R |
| Blistering, Bare Steel Corrosion from Scribe,mm Adhesion, psi, Elcometer | None 4.0 >2000 | Xylene | C |
| Note: Applied at 2-mil blast profile, KTA-Tator panels. No primer. |  |  |  |